## Slide 1
« The new intelligent sheet »
Green house effect/ IR
Noise
Noise
AKYVER® Silence
Light

## Slide 2
AKYVER® Silence
Your advantages:
Best sound reduction, till 10 dB* (Rw)
Better behaviour on rain noise, till 11 dB * (Lia)
1. Outstanding sound insulation
2. Diffusing natural light
3. Reduction of green house effect by better solar factor
4. Improved fire resistance
5. A unique aesthetic
European
Patent!
* Measures CSTB done on sheet of 20 mm with and without beads

## Slide 3
Description:
Cellular polycarbonate sheets filled with 1000µ glass beads
Available on our products:
~ Sheets in AKYVER ® 16 mm and 20 mm
~ Systems (ex: AKYVER® Panel 40- 8W)
~ Others on demand
    AKYVER ® Silence
AKYVER® Silence

## Slide 4
Sound improvement:
Filling
AKYVER® 16-7 Silence *
AKYVER® 20-7 Silence *
Rw
Sound reduction
(dB)
Rw=28
Rw=30
Lia
Rain noise
(dB)
AKYVER® Sun Type 16 7 *
Rw=20
Glass 4-16-4
SPC 16 3P + Aerogel *
Rw=21
64
73
65
-
Rw=30
62
* Measures or following CSTB technical approval
To the ear, reducing the level of 10 dB represents twice less noise
The microbeads provide an acoustic performance close to a standard double glazed
Nota:
Exterior noise: Rw index (C, Ctr) expressed in dB
The higher this index is, the less the noise disturbs the activity inside the building
Rain noise: Lia index expressed in dB.
The lower this index is, the less the noise disturbs the activity inside the building
AKYVER® Silence

## Slide 5
Light and energy improvement:
Purely indicative, being validated in the laboratory, (2) Datas from CSTB technical approval
The microbeads provide a good light scattering and limit the warming inside the premises
Nota:
LT: The higher the value is, the more the light passes through the filling and thus illuminates a room. The notion of diffusion is not considered in this index
g-W: The lower this index is, the less the sun radiations warm up a place
<1,8 à 1,9 (2)
Following the methods of measure
Filling
AKYVER® 20-7 Silence (1)
Light Transmission
LT (%)
46
Solar Factor (g-Wert)
0,43
64
0,66
Glass 4-16-4
80
0,63
SPC 16 3P + Aerogel (2)
54
0,52
AKYVER® 16-7 Silence (1)
AKYVER® Sun Type 16-7 Opale (1)
~ 50
0,49
Thermal insulation
U (W/m².K) (U-Wert)
~ 1,8
< 1,8
1,5
1,5
2,2
AKYVER® Silence

## Slide 6
Weight of fillings:
Filling
AKYVER® 20-7 Silence (1)
Weight (Kg/m²)
AKYVER® Sun Type 16 Seven
2,6
Glass 4-16-4
20
SPC 16 3W + Aerogel
3,6
~ 6,4
7,4
AKYVER® 16-7 Silence (1)
Significant weight gain in comparison
with a double glazing :
  Easier handling
  Less Fragile
Estimation by internal measuring,
AKYVER® Silence

## Slide 7
~ Bendable 150 x thickness
~ Improved fire reaction by reducing the flame spread
~ Operating temperature: -40 à +110°C
~ Light effect possible (Office separators; stand; etc...)
~ Lighter supporting structure comparing to glass installation
Warning: possible only in cut-to-size dimensions, on order
=> Filling up in the factory
Other characteristics:
AKYVER® Silence

## Slide 8
AKYVER® Silence

## Slide 9
Solar factor g
G-Wert
Thermal insulation U
(W/m²°K)
Outstanding energy and accoustic results
Sound insulation
AKYVER® Silence offer you: